Iron Luristan Swords: Literature Evaluation with links to papers

H. Föll

This is a collection of notes I made (in mixed languages).from  2017 -  2019 while pursuing the Luristan Project.  I was interested in the mask swords and trying to find answers to the questions enumerated below.

Later I run into what is called here “Dubai” swords. They are also mentioned in the Luristan modules of the Hyperscript where they are named “type 2” iron swords from Luristan.

Here is a visual definition of the “Dubai” or type 2 type sword:

The list is in chronological order. Cursive parts are from an older evaluation

Links lead to pdf copies of the papers evaluated

This evaluation looks in particular for answers to the following questions:

- How old are the “Iron Mask Swords”? Age determined how? Time line in development?

- Macroscopic structure? Made from how many parts? Assembly method? Time line in macroscopic structure development? X-rays taken?

- Microscopic structure? Composition (carbon, phosphorous, ...), Microstructure and thermal history, starting material (bloom quality), forge welding used, inclusions, ....

- Making of figures? Casting, swaging, carving, ...

- Stylistic connections.  Relation to other artifacts from Luristan; from elsewhere. Where is the “true” origin of those swords?

| 1957 | F. K. Naumann: Untersuchung eine eisernen luristanischen Kurzschwertes Archiv für das Eisenhüttenwesen, 28. Jahrgang, Heft 9, (1957) 575 - 581 |
| --- | --- |
|  | Key publication |
|  | Detailed and very good; X-ray (actually ( from Ir Isotope 15 MeV Betatron), metallograpy, chemistry. Forged, not cast. Compound construction. Older publ. assumed casting. Sword from Hamburg Museum Kunst Gewerbe. Sculptures mostly gone (“könnte sich um ein Tier handeln”) Minimal 10 individual parts; rivets Tricky “Schliff Technik”; very small area. Ferrite, some pearlite, slag inclusions, forging direction Figures not soldered on. Checked if blade was fire welded, but does not comment on it. „Fragen zur Herstellung der Figuren mussten offen bleiben“ Advocates urgently more detailed (destructive) analysis. |
|  | Contains almost everything relevant plus proper questions. Deplores reluctance of archaeologists to „destruct“ specimen |
|  | Gießen war unterstellt; Anbindung an China? HH Schwert. X-ray with Ir isotope and 15 MeV betatron. . Minimum of 10 parts. Pictures in pdf copy very bad. Microstructural test of figure for cast iron. Result: Forged bloomery wrought iron. No soldering with other metals. About 5 mm piece of blade investigated to se if fire welding occurred. Many slag inclusions. Widmannstätten ferrite, spheroidal pearlite, Blade „kunstlos“ hergestellt; not clear if fire welding. Changing carbon content, around 0.1 % average. Some questions remain open. |
| 1 How old? | „Mindestens 7. Jhdt v.C. since Luristan “ends” 600 BC |
| 2 Macroscopic structure? | Indirect data |
| 3 Microscopic structure? | Extensive X-ray (Betatron, Ir-() and Metallography. Good results (see above). Can’t decide about fire welding: |
| 4 Making of figures? | No comment but sees the problem („wäre auf Gusseisen zu prüfen”) |
| 5 Stylistic connections? | No comment (except to questionable others) |

| 1961 | Herbert Maryon; with technical reports by R. M. Organ, O. W. Ellis, R. M. Brick, R. Sneyers, E. E. Herzfeldand F. K. Naumann: Early Near Eastern Steel Swords, ´ American Journal of Archaeology, Vol. 65, No. 2 (Apr., 1961), pp. 173-184 |
| --- | --- |
|  | Key publication |
|  | Some quotes: |
|  | “Probably Shalmaneser I, King of Assyria. "As to the good iron about which thou hast written to me. Good iron is not available in my sealed store-house in Kizzuwadna. It is a bad time for producing iron. I have written that they should produce some good iron. So far they have not finished it. When they have finished I will send it to you. To-day however I have sent you a dagger- blade of iron." Kizzuwadna, it is now agreed, was situated in Cilicia. The letter proves that iron weapons were still rare, and that even at this period, the thirteenth century before Christ, the king of the Hittites had no easy access to supplies of smelted iron”. |
|  | “In recent years a number of finely designed steel daggers or short swords, all having their hilts decorated with human heads and figures of crouching lions, dating from some unknown early period, have found their way from the Near East into various collections. No closely comparable material is known, and their place of origin has not been exactly ascertained, though a number of the weapons have been found in tombs in Luristan”. |
|  | “The iron daggers are indeed a foreign element among Luristan bronzes, and though only one of the specimens is known to have come from Pontus, that must be the original provenance of them all. In Pontus, iron, easily workable, lies above ground.” |
|  | “Although these works are generally recorded as coming from Luristan there is no evidence to show that they were made there. A characteristic feature of so many of the early works found in Luristan is that their makers were interested in the casting of bronze rather than the forging of iron |
|  | “Although there is a superficial resemblance between all the known specimens of these swords, yet if they are closely examined no two are found to be quite alike.” |
|  | “The formation of the lions and of the human heads would have been effected first by forging, then the finer details would be added by means of chasing tools and punches, for there is no indication of the employment of cutting tools upon them.” |
|  | “The omission of hardening treatment on this weapon suggests that it was probably made before 900 BC.” |
|  | “Just as the earliest books printed with moveable type are in many ways unsurpassed, so here, the sword handles forged in the new metal, steel, by these pioneer smiths of the Near East, exhibit skill of a high order, and no comparable steel sword-hilts have been found in any other land before the time of the Renaissance in sixteenth century Europe.”. |
|  | Gives story of discovery Reasons why not made with dies |
|  | Gives long quotes of earlier examinations Some metallographic pictures |
|  | Reviews findings from 11 swords. Many microstructure picture, good quality X-ray pics from 1957 Naumann. “However, in the extremely smooth, level and true surfaces between the transverse ridges on the handles of these swords (pl. 65, fig. 6) we seem to have evidence for the use of the "flatter." This is a smith's tool, a solidly- made steel punch, employed with a handle made from an iron rod (or perhaps, in early times, a withy). The tool has a flat face, perhaps 1/2 inch square. It is held upon the red-hot work and blows are struck on it either by the smith or his helper”. “the weapons were forged individually, though from a single design”. “It is evident that at the time when they were being manufactured some very efficient workshops must have been available, and that the separate parts of the weapons were mass produced. The sword may have been worn as a badge of honour, awarded perhaps to some distinguished company of warriors for a notable deed of valour.“ |
| 1 How old? | Probably made before 900 BC because hardening was not used. Mass produce, “100s have been seen by some consul” |
| 2 Macroscopic structure? | Not much |
| 3 Microscopic structure? | Extensive metallography. No hardening, no mention of fire welding |
| 4 Making of figures? | Not cast or swaged, “carved”. |
| 5 Stylistic connections? | Refers to pre-Luristan sword from the “pontus”: “The modern history of these weapons begins with Herzfeld's discovery at Leningrad, in 1935, of a catalogue of the Khanenko collection at Kiev, Russia, in which reference was made to a dagger, said to be of iron, which was in that collection. Herzfeld made a special journey to see the piece in question. Of it he wrote "It is the identical dagger, from the same mould, acquired at Samsun, east of Sinope, before 90oo-I believe about 890o. No such dagger had come from Luristan before 1930, and the Khanenko piece was certainly not brought from Luristan to Samsun before 900oo, but was found in one of the many tumuli of that region of Pontus. The iron daggers are indeed a foreign element among Luristan bronzes, and though only one of the specimens is known to have come from Pontus, that must be the original provenance of them all. In Pontus, iron, easily workable, lies above ground.” |

| 1964 | Kate C. Lefferts: Technical Notes on Another Luristan Iron Sword |
| --- | --- |
|  | American Journal of Archaeology, Vol. 68, No. 1 (Jan., 1964), pp. 59-62 |
|  | Augments Maryon 1961. Best preserved ornaments; unique with 64 carnelian inlays |
|  | “It could be that the main parts of the swords were hand-forged and so have varied proportions, but that the sophisticated ornaments, which are of lower carbon content, were formed by swaging“ |
|  | Metropolitan sword. “Disregarding rivets, it seems probable that our sword was made in nine, ten, or eleven parts”. “Etching with 5% nital gave us a spheroidized carbide in ferrite structure”. “It could be that the main parts of the swords were hand-forged and so have varied proportions, but that the sophisticated ornaments, which are of lower carbon content, were formed by swaging” Bad X-ray, plenty of slag inclusions |
| 1 How old? | No info |
| 2 Macroscopic structure? | (Bad) X-ray, some metallography, 9 – 11 parts |
| 3 Microscopic structure? | Some metallography. Assumes “carburization” |
| 4 Making of figures? | “It could be that the main parts of the swords were hand-forged and so have varied proportions, but that the sophisticated ornaments, which are of lower carbon content, were formed by swaging.” |
| 5 Stylistic connections? | No info |

| 1966 | K. R. Maxwell-Hyslop and H. W. M. Hodges: Three Iron Swords from Luristan |
| --- | --- |
|  | Iraq, Vol. 28, No. 2 (Autumn, 1966), pp. 164-176 |
|  | Evidence for “Bronze leaving”? |
|  | “It is, therefore, quite possible that all the iron swords discussed here could have been made within the eleventh century B.C.“ Discusses in detail possible relations with 11th century empires. |
|  | Good X-ray and cut picture. Spheroidal cementite, large slag inclusions, good microstructure pictures. It is precisely the incompetence of the smiths that is so interesting: they had so obviously not fully realized the potentialities of the metal they were working. In fact, when one looks critically at the methods of manufacture employed-the use of flanges to hold insets, the punch technique of decoration, and the final planishing -one is reminded as much, if not more, of the bronze smith than the blacksmith.” |
|  | Analyzes 3 swords; one of them with figures. The picture below contains only sword No. 1 and 2 |

|  | 6 (=No 2) is the “famous” one |
| --- | --- |

| 1 How old? | Blade and grip of 3 are single piece of metal |
| --- | --- |
| 2 Macroscopic structure? | 11 th centuy BC quite possibly |
| 3 Microscopic structure? | Forged from single bar of metal, No heat welding in evidence. “incompetent black smiths!” |
| 4 Making of figures? | Extensive metallography as in “Bird” next page, Welding line visible belpw? |
| 5 Stylistic connections? | Not much mentioning |
|  | No obvious ancestry or progeny. But the “lions” are not uncommon, refers to this picture. |

| 1968 | Vera Bird and Henry Hodges: A METALLURGICAL EXAMINATION OF TWO EARLY IRON SWORDS FROM LURISTAN |
| --- | --- |
|  | Studies in Conservation, 13 (1968), 215-223 215 |
|  | Key Publication, gives details to the 1966 Hyslop publication |
|  | Contains good X-ray and complete sectioning of handle- Good microstructure pictures |
|  | “Two iron swords from Luristan were examined by x-ray s and using metallographic sections. The first sword was shown to have a hilt made of five pieces of metal joined by four rivets, while the pommel was secured by a dowel on the end of the tang. Hilt and blade were sectioned for metallographic study. This showed that while the core of each part was pearlite, decarburization had taken place at the surfaces to give ferritic structures.. The second sword was shown to have been made of seven pieces. The pommel was secured as in the first sword, but all other pieces were joined by fitting into prepared slots, the edges of which were burred. A section was cut from the hilt at a point where a decorative band had been applied. This showed large-grained ferrite at the surface.” Contain the good X-ray and cut pictures in Hyperscript. Discusses earlier studies, wrought iron vs. steel. Sword 1 varies from hypereutectoid to wrought iron |
|  | Discusses wrought iron vs. steel, “case hardening” etc. Presents a number of structure pictures |
|  | “All the evidence taken together would suggest that he early craftsmen who made these weapons w ere still far from arriving at any real appreciation of the nature of the raw materials they were using, and the fact that steel was present amongst their products does not mean either that it was formed deliberately or that, having made it, they knew h4ow to use it to advantage |
| 1 How old? | “Currently dated between the 12th and 7th century BC” |
| 2 Macroscopic structure? | Some discussion to the making |
| 3 Microscopic structure? | Detailed metallography, discusses (often high) carbon content |
| 4 Making of figures? | No info |
| 5 Stylistic connections? | No info |

| 1971 | C. S. Smith: The Techniques of the Luristan Smith |
| --- | --- |
|  | Science and Archaeology (Ed. Rober H. Brill), Cambridge, Massachusetss, 1971 |
|  | Substantial metallographic analysis but only 1 “real” Luri among 8 specimen. Uses electrolytic cleaning |
|  | Found strongly varying C concentration. High T working (bloom compacting?) followed by lower T deformation (forging?) Cut Luri in many parts Swords are astonishing, Hyslop is wrong Randomly varying carbon, Discusses spheroidization |
| 1 How old? | 8 century BC |
| 2 Macroscopic structure? | Welding / faggoting possibly at bloom level, but not later |
| 3 Microscopic structure? | “Smiths had not learned to hammer weld”. Hammeing with the help of swages |
| 4 Making of figures? | Heads “finished by both chiseling and chasing”, “some use of abrasives” |
| 5 Stylistic connections? | No info |

| 1971 | P. R. S. MOOREY: CATALOGUE OF THE ANCIENT PERSIAN BRONZES IN THE ASHMOLEAN MUSEUM |
| --- | --- |
|  | The book is not available: the link leads to relevant parts of it |
|  | The bearded male heads, wearing a flat cap, are not a motif found on the distinctive cast-bronzework of Luristan. The lions' heads emerging from the back of the human heads is a very unusual feature. It is these beasts, which indicate that swords of this type were probably not manufactured before the later ninth or early eighth century H.C. The parts worked over became carburized during the frequent heating process and took on the pattern of mild steel. Each sword was made of a number of separate pieces; as many as eleven in some cases. Hodges has provided an excellent diagram of the way in which these weapons were assembled from the various components (Iraq, XXVIII, 1966, pp. 175-6, fig. 2). The ornaments were attached to the main body of the sword by a combination of locking and crimping, not by heat welding. Manufacture by swaging is the most reasonable explanation for the close similarity between the ornamental fittings on these swords. This technique of hammering heated metal into a mould, used to shape wrought-iron objects before the process of smelting was developed, was of some antiquity (Przeworski, Die Metallindustrie Anatoliens in der Zeit von ISOO-JOO, p. 160). |
|  | “Methods of manufacture had been refined by the time the large series with deeorated pommels and guards were put into production, but they still mark a very early stage in the development of iron teehnology” |
| 1 | How old? | Later ninth or early eighth century |
| 2 | Macroscopic structure? | No |
| 3 | Microscopic structure? |  |
| 4 | Making of figures? | Manufacture by swaging |
| 5 | Stylistic connections? | Rather not, but a few vague hints |

| 1973 | E. Schumacher: Eisenschwerter mit Maskenzier aus Luristan Kleemann Festschrift II Teil (= Bonner Hefte zur Vorgeschichte, n. 4), Bonn, 1973, p-97 ff |
| --- | --- |
|  | A Kind of review |
|  | Describes about 30 swords, drawings for 11. Includes “Dubai” kind of sword, too and includes those in discussion |
|  | ”Dubai” kind |
| 1 | How old? Discusses various dating ways, supposes 800 – 700 BC |
| 2 | Macroscopic structure? Discusses and compares many swords. No systematics for single bade – blade inserted grip variants. |
| 3 | Microscopic structure? Clean carbon steel or wrought iron |
| 4 | Making of figures? Believes in “Gesenkschmieden” (swaging) |
| 5 | Stylistic connections? Discusses some but no pictures and not very clear. |

| 1987 | Claude Forrieres, Étude par microscopie électronique de structures de trempe d'une lame d'épée du Luristan, Étude par microscopie électronique de structures de trempe d'une lame d'épée du Luristan |
| --- | --- |
|  | ArchéoSciences, revue d'Archéométrie Année 1987 11 pp. 17-29 |
|  | Unfortunately written in a language I can’t quite relate to. |
|  | Finds 0.8 % carbon. Assumes cycling between > 1000 and < 700 oC (??) |
|  | Several good TEM micrographs Gives TTT diagram but not clear what for |
|  | Smith was quite skilled |
| 1 | How old? | ? |
| 2 | Macroscopic structure? | ? |
| 3 | Microscopic structure? | Yes |
| 4 | Making of figures? | ? |
| 5 | Stylistic connections? | ? |

| 1988 | O. Muscarella: "Bronze and Iron", New York 1988 (pp 184 . 189) |
| --- | --- |
|  | Detailed analysis of the literature and what Muscarella believd himself. No new data |
|  | Discusses the “famous” Met sword with the carnelian inlays in his usual authoritative and very detailed style. Quotes everybody and citizens incorrect colleagues. The quote belows speak for themselves |
|  | 1 How old? 750 – 650 BC 2 Macroscopic structure? Many parts, good discussion 3 Microscopic structure? No own results, Discusses wrought iron vs. steel. 4 Making of figures? Stay vague but inclines to swaging 5 Stylistic connections? Give many possible connections but without figure, |

| 1991 | J. E. Rehder, The Decorated Iron Swords From Luristan: There Material And Manufacture; Journal of Persian Studies, Iran, Vol. 29 (1991) pp. 13 - 19 |
| --- | --- |
|  | Discusses “Toronto” sword and others, including the radiocarbon dating of the Toronto and MIT sword. Arrives at 1100 BC as best age estimation. No pictrues |
|  | Reviews the available information; mentions spheroid zed cementite |
|  | Points out erroneous or misguided stuff in older publications. Marvels at workmanship but swords are not good as weapons. |
|  | Discuses smelting techniques and iron / carbon systematic. Mentions cast iron production as possible but useless. |
|  | Puts things in perspective: Couldn’t agree more. Remarks on varying carbon content and annealing. No quench hardening although it ould hav ebeen possibel |
| 1 | How old? | 1100 BC |
| 2 | Macroscopic structure? | Discussed for several swords |
| 3 | Microscopic structure? | Discussed in some detail |
| 4 | Making of figures? | Not discussed |
| 5 | Stylistic connections? | Not discussed |

| 1991 | P.R.S. Moorey> The Decorated Ironwork of the Early Iron Age Attributed to Luristan in Western Iran |
| --- | --- |
|  | In depth discussion of early iron dating problem relations in style. Many new points but no break.through |
| 1 | How old? | Lengthy discussion, valuable. Falls for C14 dating for Luri type 1 swords-. |
| 2 | Macroscopic structure? | Little |
| 3 | Microscopic structure? | No |
| 4 | Making of figures? | Little |
| 5 | Stylistic connections? | Yes, interesting bit mot convincing |

| 2003 | Bruno Overlaet, The Early Iron Age in the Pusht-i Kuh; luristan; Acta Iranica, Vol. XXVI, 2003; selected parts of the huge volume |
| --- | --- |
|  | The ultimate about Luristan general, part of the big “Irancia” book. Detailed reports about proper excavations. |
|  | In particular important for the general time lines. |
|  | Chapter about metal objects . |
| 1 | How old? | Indiorcet 800 BC – 700 BC |
| 2 | Macroscopic structure? | Article is not about mask swords |
| 3 | Microscopic structure? |  |
| 4 | Making of figures? |  |
| 5 | Stylistic connections? |  |

| 2003 | FRANCE-LANORD, A.: 1969 La Fer en Iran au premier millenaire avant Jesus Christ. Revue d'histoire des mines and metallurgie I, 75-126. |
| --- | --- |
|  | Should be very interesting but can’t get copy. In Rehder 1991 we read : |
| 1 | How old? |  |
| 2 | Macroscopic structure? |  |
| 3 | Microscopic structure? |  |
| 4 | Making of figures? |  |
| 5 | Stylistic connections? |  |

| 2005 | Bruno Overlaet, The Chronology of the Iron Age in the Pusht-i Kuh Luristan, Irancoa Antiqua, Vol XL (2005), pp. 1 - 33 |
| --- | --- |
|  | The title says it all. The fig. Below is the key for dates. |
| 1 | How old? | 800/750 – 650 BC indirectly |
| 2 | Macroscopic structure? | The article is not about mask swords |
| 3 | Microscopic structure? |  |
| 4 | Making of figures? |  |
| 5 | Stylistic connections? |  |

| 1991 | Khorasani, Manouchehr, Bronze and iron weapons from Luristan |
| --- | --- |
|  | Nice Review, not yet fully evaluated |
| 1 | How old? |  |
| 2 | Macroscopic structure? |  |
| 3 | Microscopic structure? |  |
| 4 | Making of figures? |  |
| 5 | Stylistic connections? |  |

| 2015 | A. Hasanpur et al.; The Baba Jilan Graveyard Near Nurabad, Pisht-i Kuh,Luristan – A Prelimiary Report, Irancia Antiqua, Vol. L (2015), pp 171 -212 |
| --- | --- |
|  | Reports the only mask sword found by archaeologists, albeit not by digging. It came up by sifting through the remains of a looted graveyard. |
|  | C14 dating was used but gave no clear result for the sword. Note that the sword has a kind of chap from the sheath still attached to its tip |
|  | The drawing of the construction is taken from the literature given and does not necessarily reflect the makings of this particular sword. |
| 1 | How old? | “post quem” = earliest time = 9th century = 800 BC – 900 BC |
| 2 | Macroscopic structure? | See picture; but not ceretain |
| 3 | Microscopic structure? | no |
| 4 | Making of figures? | no |
| 5 | Stylistic connections? | no |